# Overview

This online repository provides additional data to accompany the paper:

Thermoelectric Properties of Pnma and Rocksalt SnS and SnSe

J. M. Flitcroft, I. Pallikara and J. M. Skelton

Solids 3 (1), 155-176 (2022) DOI: https://doi.org/10.3390/solids3010011

This paper is open-access and freely available to download or read online from the DOI link given in the reference above.

# Summary of Data

## Overview

This repository contains raw data for each of the five structures examined in this work, viz. Pnma SnS, Pnma SnSe, equilibrium and compressed rocksalt (RS) SnS, and RS SnSe.

The data is organised into folders for each system, labelled by the material and crystal structure. For each structure the data comprises: (1) an optimised crystal structure; (2) a lattice-dynamics calculation to determine the phonon spectra and lattice thermal conductivity; and (3) an electrical-transport calculation to determine the Seebeck coefficients, electrical conductivity and electronic thermal conductivity.

The following subsections describe the content and format of the files included for the three types of calculation.

## Optimised crystal structures

Structures are provided in the plain-text POSCAR format used by Vienna Ab initio Simulation Package (VASP) code, a description of which can be found in the online manual/Wiki.[1] The structures obtained directly from the geometry optimisations are named POSCAR.Opt.vasp. For the rocksalt structures, we also provide the primitive cells in files named PPOSCAR.Opt.vasp.

## Lattice-dynamics calculations

Data for the lattice-dynamics calculations are provided in the Phono_3_py subfolders in the folders for each model.

The lattice-dynamics and lattice thermal-conductivity calculations were performed using the Phonopy and Phono3py codes,[2, 3] which work with a mix of plain-text, YAML HDF5 and PDF files. We assume those using the data in this repository are familiar with Phono(3)py. The Phonopy and Phono3py input and output files included in the repository are briefly summarised in the following two tables, and further information can be found in the online documentation for the codes.[2, 3]

For convenience, thermal-conductivity curves extracted from the main Phono3py output files are provided as CSV files, which can be easily loaded into spreadsheet software such as Excel for visualisation and/or read into scripts/programs for further processing.

The lattice-dynamics and thermal-conductivity calculations for Pnma SnS and SnSe were taken from a previous study, and the data is available in the associated repository.[4] Note, however, that the crystal structure axes are different, and the components of the thermal-conductivity tensors need to be permuted to match - for the diagonal elements, the permutations are xx → yy, yy → zz, zz → xx.

| File | Format | Description |
| --- | --- | --- |
| phonopy_disp.yaml | YAML | Metadata from the Phonopy setup. |
| FORCE_SETS | Text | Sets of atomic forces used to derive the second-order force constants. |
| projected_dos.dat | Text | Atom-projected phonon density of states 𝑔(𝑓) (PDoS) calculated using the tetrahedron method. |
| band.yaml | YAML | Phonon dispersions data. |
| band_dos.pdf | PDF | Plot of the phonon dispersion and PDoS. |

| File/Folder | Format | Description |
| --- | --- | --- |
| disp_fc3.yaml phono3py_disp.yaml | YAML | Metadata from the Phono3py setup. |
| FORCES_FC3 fc2.hdf5 fc3.hdf5 fc2.phono3py.hdf5 | Text/HDF5 | Sets of atomic forces and calculated 2nd-/3rd-order force constants. Two sets of 2nd-order FCs are provided: one from the Phonopy calculation (fc2.hdf5), and one from the Phono3py calculation (fc2.Phono3py.hdf5). The former is used in the post-processing to obtain the thermal conductivity. |
| kappa-m*.hdf5 | HDF5 | Main output file from the thermal-conductivity calculations. |
| kappa-m*.csv | CSV | Thermal-conductivity as a function of temperature extracted from the kappa-m*.hdf5 files. |

## Electrical-transport calculations

Data for the electrical-transport calculations are provided in the AMSET subfolders in the folders for each model.

These calculations were performed using the AMSET code,[5] which works with a mix of XML, HDF5 and YAML files. We again assume those using the data in this repository are familiar with AMSET. The AMSET input and output files included in the repository are briefly summarised in the following table, and further information can be found in the AMSET online documentation.[5]

| File | Format | Description |
| --- | --- | --- |
| vasprun.xml | XML | vasprun.xml file containing electronic band energies from the dense uniform band structure calculation. |
| deformation.h5 | HDF5 | Band deformation potentials. |
| wavefuncation.h5 | HDF5 | Wavefunction extracted from the VASP WAVECAR file produced during the dense uniform band structure calculation. |
| settings.yaml | YAML | Calculation settings, including materials parameters, for the AMSET runs. |

# References

- https://www.vasp.at/wiki/index.php/The_VASP_Manual (accessed 15/08/2024)

- https://phonopy.github.io/phonopy (accessed 15/08/2024)

- https://phonopy.github.io/phono3py (accessed 15/08/2024)

- https://doi.org/10.17632/hrzkm56zw7 (accessed 15/08/2024)

- https://hackingmaterials.lbl.gov/amset/ (accessed 15/08/2024)